SECTION 09 30 23 GLASS TILING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Glass tile.

          - Waterproof membrane[ for thinset applications].

        - Related Requirements:

          - Section 07 92 00 "Joint Sealants" for sealing of expansion, contraction, control, and isolation joints in tile surfaces.

Delete first option in subparagraph below if cementitious backer units are specified in this Section. See the Evaluations.

          - Section 09 29 00 "Gypsum Board" for [cementitious backer units] [glass-mat, water-resistant backer board].

      - DEFINITIONS

        - General: Definitions in the ANSI A108 series of tile installation standards and in ANSI A137.2 apply to Work of this Section unless otherwise specified.

        - ANSI A108 Series: ANSI A108.01, ANSI A108.02, ANSI A108.1A, ANSI A108.1B, ANSI A108.1C, ANSI A108.4, ANSI A108.5, ANSI A108.6, ANSI A108.8, ANSI A108.9, ANSI A108.10, ANSI A108.11, ANSI A108.12, ANSI A108.13, ANSI A108.14, ANSI A108.15, ANSI A108.16, and ANSI A108.17, which are contained in its "Specifications for Installation of Ceramic Tile."

        - ISO 13007 Standards for Ceramic Tile Grouts and Adhesives.

        - Module Size: Actual tile size plus joint width indicated.

        - Face Size: Actual tile size, excluding spacer lugs.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at Project site.

          - Review requirements in ANSI A108.01 for substrates and for preparation by other trades.

      - SUBMITTALS

        - Product Data: For each type of product.

Retain "Shop Drawings" Paragraph below if tile installations are complex enough to justify Shop Drawings.

        - Shop Drawings: Show locations of each type of tile and tile pattern. Show widths, details, and locations of expansion, contraction, control, and isolation joints in tile substrates and finished tile surfaces.

        - Samples for Initial Selection: For tile, grout, and accessories involving color selection.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above. Revise list of Samples below to correspond with products specified.

        - Samples for Verification:

Retain one of two subparagraphs below.

          - Full-size units of each type and composition of tile and for each color and finish required.[ For glass mosaic tile in color blend patterns, provide full sheets of each color blend.]

          - Assembled samples mounted on a rigid panel, with grouted joints, for each type and composition of tile and for each color and finish required. Make samples at least [12 inches (300 mm) square] [36 inches (900 mm) square], but not fewer than four tiles. Use grout of type and in color or colors approved for completed Work.

        - Qualification Data: For Installer.

        - Master Grade Certificates: For each shipment, type, and composition of tile, signed by tile manufacturer and Installer.

        - Product Certificates: For each type of product.

        - Product Test Reports: For tile-setting and -grouting products.

      - QUALITY ASSURANCE

        - Installer Qualifications:

        - Installer Qualifications:  Engage an experienced installer having a minimum of 5 years of experience on projects of comparable size and scope who has completed tile installations similar in material, design, and extent to that indicated for this Project and with a record of successful in-service performance.

EDIT MOCKUP SIZE PER PROJECT REQUIREMENTS

        - Mockups: Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Build 4 feet by 8 feet mockup of each type of floor tile installation.

          - Build a full wall mockup of each type of wall tile installation.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver and store packaged materials in original containers with seals unbroken and labels intact until time of use. Comply with requirements in ANSI A137.2 for labeling tile packages.

        - Store tile and cementitious materials on elevated platforms, under cover, and in a dry location.

        - Store aggregates where grading and other required characteristics can be maintained and contamination can be avoided.

        - Store liquid materials in unopened containers and protected from freezing.

      - FIELD CONDITIONS

        - Environmental Limitations: Do not install tile until construction in spaces is complete and ambient temperature and humidity conditions are maintained at the levels indicated in referenced standards and manufacturer's written instructions.

- PRODUCTS

      - MANUFACTURERS

        - Source Limitations for Tile: Obtain tile of each type and color or finish from single source or producer.

          - Obtain tile of each type and color or finish from same production run and of consistent quality in appearance and physical properties for each contiguous area.

        - Source Limitations for Setting and Grouting Materials: Obtain ingredients of a uniform quality for each mortar, adhesive, and grout component from single manufacturer and each aggregate from single source or producer.

          - Obtain setting and grouting materials, except for unmodified Portland cement and aggregate, from single manufacturer.

          - Obtain waterproof membrane, except for sheet products, from manufacturer of setting and grouting materials.

        - Source Limitations for Other Products: Obtain each of the following products specified in this Section from a single manufacturer:

          - Waterproof membrane.

          - Metal edge strips.

      - PRODUCTS, GENERAL

        - ANSI Glass Tile Standard: Provide glass tile that complies with ANSI A137.2 for types and other characteristics indicated.

          - Provide tile complying with Standard grade requirements unless otherwise indicated.

        - ANSI Standards for Tile Installation Materials: Provide materials complying with ANSI A108.02, ANSI standards referenced in other Part 2 articles, ANSI standards referenced by TCNA installation methods specified in tile installation schedules, and other requirements specified.

        - Factory Blending: For tile exhibiting color variations within ranges, blend tile in factory and package so tile units taken from one package show same range in colors as those taken from other packages and match approved Samples.

        - Mounting: For factory-mounted tile, provide back- or edge-mounted tile assemblies as standard with manufacturer unless otherwise indicated.

Retain subparagraph below if tile is used on exteriors or in wet areas. According to ANSI A137.2, manufacturers must specify whether back- or edge-mounted tile assemblies are suitable for these installations, because mounting materials decrease contact area of setting material to tile, and mounting materials may not be as strong or as waterproof as setting materials.

          - Where tile is indicated for installation [on exteriors] [or] [in wet areas], do not use back- or edge-mounted tile assemblies unless tile manufacturer specifies in writing that this type of mounting is suitable for installation indicated and has a record of successful in-service performance.

      - TILE PRODUCTS

        - Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

          - Tile Products:

            - American Olean Tile Company.

            - Crossville Ceramics.

            - Dal-Tile Corporation.

            - Deutsche Steinzeug America, Inc.

            - Interceramic.

            - Louisville Tile.

            - Grupo Porcelanite.

            - Portobello America, Inc.

            - Seneca Tiles, Inc.

            - Thorntree Slate.

        - Basis of Design Products:  Refer to Interior Finish Legend on Drawings.

        - Colors, Textures, and Patterns:  Where manufacturer's standard products are indicated for tile, grout, and other products requiring selection of colors, surface textures, patterns, and other appearance characteristics, provide specific products or materials complying with the following requirements:

          - Provide as indicated in Interior Finish Legend, unless otherwise indicated.

        - Trim Units:  Provide tile trim units to match characteristics of adjoining flat tile and to comply with the following requirements:

          - Size:  As indicated, coordinated with sizes and coursing of adjoining flat tile where applicable.

      - WATERPROOF MEMBRANE

        - General: Manufacturer's standard product that complies with ANSI A118.10 and is recommended by the manufacturer for the application indicated. Include reinforcement and accessories recommended by manufacturer.

        - Fluid-Applied Membrane: Liquid-latex rubber or elastomeric polymer.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Laticrete International, Inc.; Laticrete Hydroban.

            - MAPEI Corporation; Mapelastic AquaDefense.

            - TEC; H.B. Fuller Construction Products Inc.; Hydra Flex Waterproofing Membrane.

      - SETTING MATERIALS

ANSI standards for glass tile installation recommend using white cement for translucent glass tile.

        - Portland Cement Mortar (Thickset) Installation Materials: ANSI A108.02; use white cement unless otherwise indicated.

          - Cleavage Membrane: Asphalt felt, ASTM D 226/D 226M, Type I (No. 15); or polyethylene sheeting, ASTM D 4397, 4.0 mils (0.1 mm) thick.

Retain "Reinforcing Wire Fabric" Subparagraph below for reinforced mortar bed.

          - Reinforcing Wire Fabric: Galvanized, welded-wire fabric, 2 by 2 inches (50.8 by 50.8 mm) by 0.062-inch (1.57-mm) diameter; comply with ASTM A 185/A 185M and ASTM A 82/A 82M, except for minimum wire size.

Retain "Expanded Metal Lath" Subparagraph below for portland cement plaster scratch coat. Delete if scratch coat is specified in Section 09 24 00 "Cement Plastering."

          - Expanded Metal Lath: Diamond-mesh lath complying with ASTM C 847.

            - Base Metal and Finish for Interior Applications: Uncoated or zinc-coated (galvanized) steel sheet, with uncoated steel sheet painted after fabrication into lath.

            - Base Metal and Finish for Exterior Applications: Zinc-coated (galvanized) steel sheet.

            - Configuration over Studs and Furring: Flat.

            - Configuration over Solid Surfaces: Self-furring.

            - Weight: [2.5 lb/sq. yd. (1.4 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

          - Polymer-Modified Thick-Bed and Render Mortar premixed, cement-based, polymer-modified thick-bed and render mortar that includes a blend of select aggregates.

            - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

              - Laticrete 3701 Fortified Mortar.

              - MAPEI Corporation “Modified Mortar Bed.”

ANSI standards for glass tile installation recommend using white cement for translucent glass tile.

        - Modified Dry-Set Cement Mortar (Thinset): ANSI A118.4 and ISO 13007; C2; white, unless otherwise indicated.

            - Wall Applications, non-large format tile:

              - Ardex Engineered Cements, “X5”.

              - Custom Building Products, “MegaLite Rapid Set Crack Prevention Mortar.”

              - Laticrete International, Inc., “253 Gold.”

              - MAPEI Corporation, “Ultraflex 2.”

RETAIN FOLLOWING SUBPARAGRAPH FOR LARGE FORMAT WALL TILE INSTALLATIONS.

FOR WALL TILE LARGER THAN 14-INCHES BY 14-INCHES.  THIS WILL HELP ASURE WALL ADHESION AND TO PREVENT CRACKING IN THE TILE.

            - Wall Applications, large format tile:

              - Ardex Engineered Cements, “X77”.

              - Custom Building Products, “ProLite”.

              - Laticrete International, Inc., Laticrete; 255 MultiMax.

              - MAPEI Corporation, “Ultralite Pro”.

              - TEC; H.B. Fuller Construction Products Inc. “3N1 Performance Mortar.

          - Provide prepackaged, dry-mortar mix combined with acrylic resin or styrene-butadiene-rubber liquid-latex additive at Project site.

          - For wall applications, provide mortar that complies with requirements for nonsagging mortar in addition to the other requirements in ANSI A118.4 and ISO 13007; C2T.

        - Water-Cleanable, Tile-Setting Epoxy: ANSI A118.3 and ISO 13007; R2.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Custom Building Products, “EBM Lite”.

            - Laticrete International, Inc., “Latapoxy 300.”

            - MAPEI Corporation, “Kerapoxy 410”.

          - Adhesives shall have a VOC content of 65 g/L or less.

          - Provide product capable of withstanding continuous and intermittent exposure to temperatures of up to 140 and 212 deg F (60 and 100 deg C), respectively, and certified by manufacturer for intended use.

      - GROUT MATERIALS

        - Standard Cement Grout (Sanded or Unsanded as Scheduled): ANSI A118.6 and ISO 13007; CG2WA.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Ardex Engineered Cements, “FH / FG-C grout”.

            - Custom Building Products, “PolyBlend Grout.”

            - Laticrete International, Inc., “1500” / “1600”.

            - MAPEI Corporation, “Keracolor S or U.”

            - TEC; H.B. Fuller Construction Products Inc. “Accucolor Sanded or Unsanded Grout”.

        - High-Performance Tile Grout: ANSI A118.7.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Ardex Engineered Cements, “FL grout”.

            - Custom Building Products, “Prism SureColor Grout.”

            - Laticrete International, Inc., “Permacolor Select” Grout.

            - MAPEI Corporation, “Ultracolor Plus” Grout

            - TEC; H.B. Fuller Construction Products Inc. “Accucolor XT”.

          - Polymer Type:  Acrylic resin or styrene-butadiene rubber in liquid-latex form for addition to prepackaged dry-grout mix.

        - Water-Cleanable Epoxy Grout: ANSI A118.3 and ISO 13007; RG, with a VOC content of 65 g/L or less.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Ardex Engineered Cements, “WA 100% solids epoxy grout”.

            - Custom Building Products, “100% Solids Epoxy Grout” or “Fusion”.

            - Laticrete International, Inc., “SpectraLOCK Pro Grout.”

            - MAPEI Corporation, “Kerapoxy CQ” or “Flexcolor CQ”.

          - Provide product capable of withstanding continuous and intermittent exposure to temperatures of up to 140 and 212 deg F (60 and 100 deg C), respectively, and certified by manufacturer for intended use.

      - MISCELLANEOUS MATERIALS

        - Trowelable Underlayments and Patching Compounds: Latex-modified, portland cement-based formulation provided or approved by manufacturer of tile-setting materials for installations indicated.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Ardex Engineered Cements, Feather Finish or K15.

            - Laticrete, “ L&M Duracrete” or “L&M Durapatch Industrial”

            - MAPEI, “Mapecem Quickpatch.”

Retain "Metal Edge Strips" Paragraph below if metal edge strips are required at junction with other finishes; revise if metal edge control joints are required.

        - Metal Edge Strips: Angle or L-shaped, height to match tile and setting-bed thickness, metallic or combination of metal and PVC or neoprene base, designed specifically for flooring applications; nickel silver or stainless-steel, ASTM A 666, 300 Series exposed-edge material.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Blanke Corporation.

            - Ceramic Tool Company, Inc.

            - Schluter Systems L.P.

EDIT AS REQUIRED TO MEET PROJECT REQUIREMENTS.

          - Basis of Design Manufacturer:  Schluter Systems.

            - Profiles:

              - Outside Corner Edge Protection, Tile-to-Tile:  QUADEC.

              - Outside Corner Edge Protection, Tile-to-Gypsum Board:  SCHIENE.

              - Finishing Edge Protection, Tile-to-Gypsum Board:  SCHIENE.

        - Tile Cleaner: A neutral cleaner capable of removing soil and residue without harming tile and grout surfaces, specifically approved for materials and installations indicated by tile and grout manufacturers.

          - Basis of Design Products, Laticrete, “Stonetech Professional Stone & Tile Cleaner”.

GROUT SEALER IS NOT REQUIRED IF YOU ARE USING EPOXY GROUT.

        - Grout Sealer: Manufacturer's standard product for sealing grout joints and that does not change color or appearance of grout.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Custom Building Products; Aqua Mix; Sealer’s Choice Gold.

            - Laticrete; StoneTech Professional Advanced Grout Sealer.

            - MAPEI Corporation, “Ultracare Penetrating Tile, Stone & Grout Sealer”.

            - Miracle Sealants Company; 511 H2O Plus Grout Sealer.

            - Merkrete, a Parex USA Inc. company, “GroutSealer”.

      - MIXING MORTARS AND GROUT

        - Mix mortars and grouts to comply with referenced standards and mortar and grout manufacturers' written instructions.

        - Add materials, water, and additives in accurate proportions.

        - Obtain and use type of mixing equipment, mixer speeds, mixing containers, mixing time, and other procedures to produce mortars and grouts of uniform quality with optimum performance characteristics for installations indicated.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions where tile will be installed, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

          - Verify that substrates for setting tile are firm; dry; clean; free of coatings that are incompatible with tile-setting materials, including curing compounds and other substances that contain soap, wax, oil, or silicone; and comply with flatness tolerances required by ANSI A108.01 for installations indicated.

          - Verify that concrete substrates for tile floors installed with [bonded mortar bed] [or] [thinset mortar] comply with surface finish requirements in ANSI A108.01 for installations indicated.

            - Verify that surfaces that received a steel trowel finish have been mechanically scarified.

            - Verify that protrusions, bumps, and ridges have been removed by sanding or grinding.

          - Verify that installation of grounds, anchors, recessed frames, electrical and mechanical units of work, and similar items located in or behind tile has been completed.

          - Verify that joints and cracks in tile substrates are coordinated with tile joint locations; if not coordinated, adjust joint locations in consultation with Architect.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Where indicated, prepare substrates to receive waterproofing by applying a reinforced mortar bed that complies with ANSI A108.1A and is sloped 1/4 inch per foot (1:50) toward drains.

        - Blending: For tile exhibiting color variations, verify that tile has been factory blended and packaged so tile units taken from one package show same range of colors as those taken from other packages and match approved Samples. If not factory blended, either return to manufacturer or blend tiles at Project site before installing.

      - GLASS TILE INSTALLATION

        - Comply with TCNA's "Handbook for Ceramic, Glass, and Stone Tile Installation" for TCNA installation methods specified in tile installation schedules. Comply with parts of the ANSI A108 series "Specifications for Installation of Ceramic Tile" that are referenced in TCNA installation methods, specified in tile installation schedules, and apply to types of setting and grouting materials used.

        - Extend tile work into recesses and under or behind equipment and fixtures to form complete covering without interruptions unless otherwise indicated. Terminate work neatly at obstructions, edges, and corners without disrupting pattern or joint alignments.

        - Accurately form intersections and returns. Perform cutting and drilling of tile without marring visible surfaces. Carefully grind cut edges of tile abutting trim, finish, or built-in items for straight aligned joints. Fit tile closely to electrical outlets, piping, fixtures, and other penetrations so plates, collars, or covers overlap tile.

If accent tile is used, verify tile thicknesses and retain first paragraph below if necessary. If difference in thickness is significant, consider providing a thicker substrate under thinner tile.

        - Where accent tile differs in thickness from field tile, vary setting-bed thickness so that tiles are flush.

        - Jointing Pattern: Lay tile in grid pattern unless otherwise indicated. Lay out tile work and center tile fields in both directions in each space or on each wall area. Lay out tile work to minimize the use of pieces that are less than half of a tile. Provide uniform joint widths unless otherwise indicated.

Retain first subparagraph below for mounted tile.

          - For tile mounted in sheets, make joints between tile sheets same width as joints within tile sheets so joints between sheets are not apparent in finished work.

        - Joint Widths: Unless otherwise indicated, install tile with the following joint widths:

Joint widths in subparagraphs below are examples only. Coordinate joint widths with grout selections and module sizes specified in "Tile Products" Article.

          - Large Format Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)].

          - Mosaic Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)].

          - Miniature Mosaic Glass Tile: [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)].

Retain first paragraph below for wainscots. Verify that instruction agrees with detailing.

        - Lay out tile wainscots to dimensions indicated or to next full tile beyond dimensions indicated.

Refer to TCNA's "Handbook for Ceramic, Glass, and Stone Tile Installation" and to the ANSI A108 series of tile installation standards for data on expansion joints. These standards require that joint locations be indicated on Drawings.

        - Expansion Joints: Provide expansion joints and other sealant-filled joints, including control, contraction, and isolation joints, where indicated. Form joints during installation of setting materials, mortar beds, and tile. Do not saw-cut joints after installing tiles.

          - Where joints occur in concrete substrates, locate joints in tile surfaces directly above them.

        - Metal Edge Strips: Install at locations indicated.

        - Grout Sealer: Apply grout sealer to grout joints according to grout-sealer manufacturer's written instructions. As soon as grout sealer has penetrated grout joints, remove excess sealer and sealer from tile faces by wiping with soft cloth.

      - WATERPROOFING INSTALLATION

        - Install waterproofing to comply with ANSI A108.13 and manufacturer's written instructions to produce waterproof membrane of uniform thickness that is bonded securely to substrate.

        - Allow waterproofing to cure and verify by testing that it is watertight before installing tile or setting materials over it.

      - CLEANING AND PROTECTING

        - Cleaning: On completion of placement and grouting, clean all tile surfaces so they are free of foreign matter.

          - Remove grout residue from tile as soon as possible.

          - Clean grout smears and haze from tile according to tile and grout manufacturer's written instructions but no sooner than 10 days after installation. Use only cleaners recommended by tile and grout manufacturers and only after determining that cleaners are safe to use by testing on samples of tile and other surfaces to be cleaned. Protect metal surfaces and plumbing fixtures from effects of cleaning. Flush surfaces with clean water before and after cleaning.

          - Remove temporary protective coating by method recommended by coating manufacturer and that is acceptable to tile and grout manufacturer. Trap and remove coating to prevent drain clogging.

        - Protect installed tile work with kraft paper or other heavy covering during construction period to prevent staining, damage, and wear. If recommended by tile manufacturer, apply coat of neutral protective cleaner to completed tile walls.

        - Before final inspection, remove protective coverings and rinse neutral protective cleaner from tile surfaces.

      - EXTERIOR GLASS TILE INSTALLATION SCHEDULE

NOTE: THESE ARE SAMPLE INSTALLATION METHODS ONLY. EDIT AS REQUIRED.

        - Exterior Wall Installations, Masonry or Concrete:

RETAIN FOLLOWING PARAGRAPH FOR TYPICAL EXTERIOR THICK-SET GLASS TILE WALL APPLICATION.  USE THIS OR EDIT PER PROJECT REQUIREMENTS.

          - Glass Tile Installation W201: TCNA W201 and ANSI A108.14, ANSI A108.15 or ANSI A108.16; cement mortar bed (thickset) on metal lath over waterproof membrane.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Bond Coat:  Modified dry-set mortar.

            - Grout:  High-performance unsanded grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  At exterior walls at entry.

RETAIN FOLLOWING PARAGRAPH FOR TYPICAL EXTERIOR THIN-SET GLASS TILE WALL APPLICATION.  USE THIS OR EDIT PER PROJECT REQUIREMENTS.

          - Glass Tile Installation W202: TCNA W202; thinset mortar[ over waterproof membrane].

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  High-performance unsanded grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  At exterior walls.

NOTE: THESE ARE SAMPLE INSTALLATION METHODS ONLY. EDIT AS REQUIRED.

      - INTERIOR GLASS TILE INSTALLATION SCHEDULE

RETAIN THE FOLLOWING FOR THIN-SET GLASS TILE INSTALLATION ON MASONRY. USE THIS OR EDIT PER PROJECT REQUIREMENTS.

        - Interior Wall Installations, Masonry or Concrete:

          - Glass Tile Installation W202: TCNA W202; thinset mortar.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  [High-performance unsanded] [Water-cleanable epoxy] grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  Where indicated on Drawings.

        - Interior Wall Installations, Metal Studs or Furring:

RETAIN THE FOLLOWING FOR THIN-SET GLASS TILE INSTALLATION ON GYPSUM BOARD. USE THIS OR EDIT PER PROJECT REQUIREMENTS.

          - Glass Tile Installation W243: TCNA W243; thinset mortar on gypsum board.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  High-performance unsanded grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  Where indicated on Drawings.

RETAIN THE FOLLOWING FOR THIN-SET GLASS TILE WALL INSTALLATION ON COATED GLASS MAT BOARD. USE THIS OR EDIT PER PROJECT REQUIREMENTS. CAN BE USED IN WET AREAS.

          - Glass Tile Installation W248: TCNA W248; thinset mortar on glass-mat, water-resistant gypsum backer board.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  [High-performance unsanded] [Water-cleanable epoxy] grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  Shower walls.

        - Shower Receptor and Wall Installations:

RETAIN FOLLOWING SUBPARAGRAPH FOR THIN-SET GLASS TILE SHOWER INSTALLATIONS ON COATED GLASS MAT BOARD.  USE THIS OR EDIT PER PROJECT REQUIREMENTS.

          - Glass Tile Installation B420: TCNA B420; thinset mortar on waterproof membrane over coated glass-mat, water-resistant gypsum backer board.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  Water-cleanable epoxy grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  Shower walls.

RETAIN FOLLOWING SUBPARAGRAPH FOR THIN-SET GLASS TILE SHOWER INSTALLATIONS ON CEMENT BOARD WITH A WATERPROOF MEMBRANE ON THE SUBSTRATE.  USE THIS OR EDIT PER PROJECT REQUIREMENTS.

          - Glass Tile Installation B421: TCNA B421; thinset mortar on waterproof membrane over solid backing.

            - Glass Tile Type: Refer to Interior Finish Legend on Drawings.

            - Thinset Mortar:  Modified dry-set mortar.

            - Grout:  [High-performance unsanded] [Water-cleanable epoxy] grout.

EDIT BELOW TO SUIT PROJECT REQUIREMENTS.  OR SCHEDULE ON DRAWINGS.

            - Locations:  Shower walls.

END OF SECTION 09 30 23

FOR MDACC USE ONLY. DELETE THIS PAGE BEFORE ISSUING DOCUMENTS.

document revision history

| Issue | Date | Revision Description | Author |
| --- | --- | --- | --- |
|  | 30190301 | Original Issuance |  |
| Rev. 1 |  | . |  |
| Rev. 2 |  |  |  |
| Rev. 3 |  |  |  |
| Rev. 4 |  |  |  |
| Rev. 5 |  |  |  |