SECTION 09 67 23 RESINOUS FLOORING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section includes resinous flooring systems.

        - Related Sections:

          - Section 07 92 00 "Joint Sealants" for sealants installed at joints in resinous flooring systems.

      - PREINSTALLATION MEETINGS

RETAIN "PREINSTALLATION CONFERENCE" PARAGRAPH BELOW IF WORK OF THIS SECTION IS EXTENSIVE OR COMPLEX ENOUGH TO JUSTIFY A CONFERENCE.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

IF NEEDED, INSERT LIST OF CONFERENCE PARTICIPANTS NOT MENTIONED IN SECTION 013100 "PROJECT MANAGEMENT AND COORDINATION."

      - SUBMITTALS

        - Product Data:  For each type of product indicated.  Include manufacturer's technical data, application instructions, and recommendations for each resinous flooring component required.

        - Samples for Verification:  For each resinous flooring system required, 6 inches (150 mm) square, applied to a rigid backing by Installer for this Project.

        - Product Schedule:  For resinous flooring.  Use same designations indicated on Drawings.

        - Installer Certificates:  Signed by manufacturer certifying that installers comply with specified requirements.

        - Material Certificates:  For each resinous flooring component, from manufacturer.

        - Material Test Reports:  For each resinous flooring system.

        - Maintenance Data:  For resinous flooring to include in maintenance manuals.

      - QUALITY ASSURANCE

        - Installer Qualifications:  Manufacturer's authorized representative who is trained and approved for installation of flooring systems required for this Project.

          - Engage an installer who is certified in writing by resinous flooring manufacturer as qualified to apply resinous flooring systems indicated.

        - Mockups:  Apply mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Apply full-thickness mockups on 48-inch- (1200-mm-) square floor area selected by Architect.

            - Include 48-inch (1200-mm) length of integral cove base with inside and outside corner.

          - Simulate finished lighting conditions for Architect's review of mockups.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver materials in original packages and containers, with seals unbroken, bearing manufacturer's labels indicating brand name and directions for storage and mixing with other components.

      - PROJECT CONDITIONS

        - Environmental Limitations:  Comply with resinous flooring manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting resinous flooring application.

        - Lighting:  Provide permanent lighting or, if permanent lighting is not in place, simulate permanent lighting conditions during resinous flooring application.

        - Close spaces to traffic during resinous flooring application and for not less than 24 hours after application unless manufacturer recommends a longer period.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

        - Flammability:  Self-extinguishing according to ASTM D635

      - MANUFACTURERS

        - Source Limitations: Obtain primary resinous flooring materials, including primers, resins, hardening agents, grouting coats, and topcoats, from single source from single manufacturer. Obtain secondary materials, including patching and fill material, joint sealant, and repair materials, of type and from manufacturer recommended in writing by manufacturer of primary materials.

        - Basis of Design Manufacturer:  Life Science Inc.

        - Subject to compliance with requirements, provide products by indicated on Drawings or comparable products approved in writing by one of the following:

          - BASF Construction Chemicals, Inc.; BASF Building Systems.

          - Crossfield Products Corp.; Dex-O-Tex.

          - Sika.

          - Life Science Inc.

      - MATERIALS

        - VOC Content of Liquid-Applied Flooring Components:  Mot more than 100 g/L when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

      - RESINOUS FLOORING

        - Resinous Flooring System: Abrasion-, impact-, and chemical-resistant, aggregate-filled, and resin-based monolithic floor surfacing designed to produce a seamless floor[ and integral cove base].

        - System Characteristics:

          - Color and Pattern: [As selected by Architect from manufacturer's full range] [As indicated by product designation listed above] [Match Architect's sample] <Insert description>.

          - Wearing Surface: [Textured for slip resistance] [Orange-peel texture] [Smooth] [Manufacturer's standard wearing surface] <Insert description>.

          - Overall System Thickness: [20 mils (0.5 mm)] [40 mils (1.0 mm)] [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)] [3/16 inch (4.8 mm)] [1/4 inch (6.4 mm)] <Insert thickness>.

REVISE "FEDERAL AGENCY APPROVALS" SUBPARAGRAPH BELOW TO SUIT PROJECT; DELETE IF NOT REQUIRED.

          - Federal Agency Approvals: [USDA] [FDA] approved for food-processing environments.

RETAIN "PRIMER" PARAGRAPH BELOW IF PRIMER IS REQUIRED. SOME SYSTEMS ARE SELF-PRIMING. SOME MANUFACTURERS OFFER ALTERNATIVE PRIMERS.

        - Primer: Type recommended by resinous flooring manufacturer for substrate and resinous flooring system indicated.

          - Formulation Description: [100 percent solids] [High solids] [Water based] <Insert requirements>.

RETAIN "WATERPROOFING MEMBRANE" PARAGRAPH BELOW IF WATERPROOFING MEMBRANE IS REQUIRED. WATERPROOFING MEMBRANES MAY BE SELF-PRIMING, OR PRIMERS MAY BE REQUIRED OVER WATERPROOFING MEMBRANES.

        - Waterproofing Membrane: Type recommended by resinous flooring manufacturer for substrate and resinous flooring system indicated.

          - Formulation Description: [100 percent solids] [High solids] <Insert requirements>.

RETAIN "REINFORCING MEMBRANE" PARAGRAPH BELOW IF A REINFORCING MEMBRANE IS REQUIRED FOR CRACK CONTROL. REINFORCING MEMBRANES ARE TYPICALLY PLACED JUST OVER THE CRACK AREA AND NOT THE ENTIRE SUBSTRATE SURFACE. BEFORE RETAINING, VERIFY AVAILABILITY FOR SYSTEMS SELECTED. PRIMER MAY BE REQUIRED IF REINFORCING MEMBRANE IS APPLIED TO ENTIRE SUBSTRATE SURFACE.

        - Reinforcing Membrane: Flexible resin formulation that is recommended by resinous flooring manufacturer for substrate and resinous flooring system indicated and that inhibits substrate cracks from reflecting through resinous flooring.

          - Formulation Description: [100 percent solids] [High solids] <Insert requirements>.

RETAIN SUBPARAGRAPH BELOW IF REQUIRED, OR REVISE TO SUIT PRODUCTS SELECTED. FIBERGLASS-SCRIM REINFORCEMENT MAY NOT BE REQUIRED IN AREAS SUBJECT TO MODERATE IMPACT; CONSULT MANUFACTURERS FOR RECOMMENDATIONS.

            - Provide fiberglass scrim embedded in reinforcing membrane.

        - Patching and Fill Material: Resinous product of or approved by resinous flooring manufacturer and recommended by manufacturer for application indicated.

        - Body Coats:

          - Resin: [Epoxy] [Urethane] [Epoxy novolac] [Vinyl ester] [Methyl methacrylate] [Polyaspartic] <Insert resin>.

          - Formulation Description: [100 percent solids] [High solids] [Water based] <Insert requirements>.

          - Type: [Clear] [Pigmented] <Insert description>.

          - Application Method: [Self-leveling slurry with broadcast aggregates] [Self-leveling slurry] [Troweled or screeded].

          - Number of Coats: [One] [Two] <Insert number>.

          - Thickness of Coats: [8 mils (0.2 mm)] [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)] <Insert thickness>.

          - Aggregates: [Manufacturer's standard] [Colored quartz (ceramic-coated silica)] [Vinyl flakes] [Granite] [Natural silica] <Insert requirements>.

RETAIN "GROUT COAT" PARAGRAPH BELOW IF REQUIRED; NOT ALL SYSTEMS REQUIRE A GROUT COAT.

        - Grout Coat:

          - Resin: [Epoxy] [Urethane] [Epoxy novolac] [Vinyl ester] [Methyl methacrylate] [Polyaspartic] <Insert resin>.

          - Formulation Description: [100 percent solids] [High solids] [Water based] <Insert requirements>.

          - Type: [Clear] [Pigmented] <Insert description>.

          - Thickness of Coat: [8 mils (0.2 mm)] [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)] <Insert thickness>.

VARIOUS TOPCOAT OPTIONS ARE AVAILABLE FOR RESINOUS FLOORING SYSTEMS. REVISE "TOPCOATS" PARAGRAPH BELOW TO SUIT PROJECT.

        - Topcoats: Sealing or finish coats.

          - Resin: [Epoxy] [Urethane] [Epoxy novolac] [Vinyl ester] [Methyl methacrylate] [Polyaspartic] <Insert resin>.

          - Formulation Description: [100 percent solids] [High solids] [Water based] <Insert requirements>.

          - Type: [Clear] [Pigmented] <Insert description>.

          - Number of Coats: [One] [Two] <Insert number>.

          - Thickness of Coats: [8 mils (0.2 mm)] [1/16 inch (1.6 mm)] [1/8 inch (3.2 mm)] <Insert thickness>.

          - Finish: [Matte] [Gloss].

IF NECESSARY, INSERT REQUIREMENTS FOR METAL OR PLASTIC COVE CAPS FOR INTEGRAL COVE BASE OR OTHER MATERIALS REQUIRED FOR RESINOUS FLOORING SYSTEMS SELECTED.

RETAIN "SYSTEM PHYSICAL PROPERTIES" PARAGRAPH BELOW AND INSERT VALUES TO ESTABLISH CRITERIA FOR SYSTEM PHYSICAL PROPERTIES IF REQUIRED. MANUFACTURERS' TESTING PROCEDURES DIFFER; REVISE TEST METHODS INDICATED AND INSERT ADDITIONAL REQUIREMENTS TO SUIT PROJECT.

        - System Physical Properties: Provide resinous flooring system with the following minimum physical property requirements when tested according to test methods indicated:

SUBPARAGRAPHS BELOW ARE EXAMPLES ONLY AND ARE BASED ON TEST METHODS REQUIRED IN ASTM C722 AND MIL-D-3134J. REVISE TO SUIT PROJECT.

          - Compressive Strength: <Insert value> minimum according to ASTM C579.

          - Tensile Strength: <Insert value> minimum according to ASTM C307.

          - Flexural Modulus of Elasticity: <Insert value> minimum according to ASTM C580.

          - Water Absorption: <Insert number> percent maximum according to ASTM C413.

          - Shrinkage: <Insert number> percent maximum according to ASTM C531.

          - Indentation: <Insert number> percent maximum according to MIL-D-3134J.

          - Impact Resistance: No chipping, cracking, or delamination and not more than 1/16-inch (1.6-mm) permanent indentation according to MIL-D-3134J.

          - Resistance to Elevated Temperature: No slip or flow of more than 1/16 inch (1.6 mm) according to MIL-D-3134J.

          - Abrasion Resistance: <Insert value> maximum weight loss according to ASTM D4060.

          - Hardness: <Insert value>, Shore D according to ASTM D2240.

IF REQUIRED BY AUTHORITIES HAVING JURISDICTION OR OWNER, INSERT FIRE-TEST-RESPONSE-CHARACTERISTIC REQUIREMENTS TO SUIT PROJECT. RETAIN FIRST OPTION IN "CRITICAL RADIANT FLUX" SUBPARAGRAPH BELOW IF CLASS I FLOOR FINISH MATERIALS ARE REQUIRED; RETAIN SECOND OPTION IF CLASS II FLOOR FINISH MATERIALS ARE REQUIRED. SEE "FIRE-TEST-RESPONSE CHARACTERISTICS" ARTICLE IN THE EVALUATIONS.

          - Critical Radiant Flux: [0.45 W/sq. cm] [0.22 W/sq. cm] or greater according to NFPA 253.

RETAIN "SYSTEM CHEMICAL RESISTANCE" PARAGRAPH BELOW TO ESTABLISH CRITERIA FOR CHEMICAL RESISTANCE. IF RETAINING, AND IF CRITERIA APPLY ONLY TO SYSTEM'S TOPCOAT, REVISE TO SUIT PROJECT.

        - System Chemical Resistance: Test specimens of cured resinous flooring system are unaffected when tested according to [ASTM D1308 for 50 percent immersion] [ASTM D543, Procedure A, for immersion] [ASTM C267 for immersion] <Insert testing requirements> in the following reagents for no fewer than seven days:

          - <Insert list of reagents that Owner has determined are likely to contact resinous flooring during in-service use>.

      - ACCESSORIES

        - Primer:  Type recommended by manufacturer for substrate and body coats indicated.

          - Formulation Description:  100 percent solids.

        - Patching and Fill Material:  Resinous product of or approved by resinous flooring manufacturer and recommended by manufacturer for application indicated.

        - Crack Repair: Two-component flexibilized epoxy crack and joint treatment to be used exclusively for the isolation of dynamic cracks.  To be used in conjunction with 10 oz. fiberglass reinforcing fabric as necessary.

        - Joint Sealant:  Type recommended or produced by resinous flooring manufacturer for type of service and joint condition indicated.

        - Trim Accessories:

          - Zinc integral cove strip and cap strip.

          - Zinc flooring transition / divider strip.

- EXECUTION

      - PREPARATION

        - General:  Prepare and clean substrates according to resinous flooring manufacturer's written instructions for substrate indicated.  Provide clean, dry substrate for resinous flooring application.

        - Concrete Substrates:  Provide sound concrete surfaces free of laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants incompatible with resinous flooring.

          - Roughen concrete substrates as follows:

            - Comply with ASTM C 811 requirements unless manufacturer's written instructions are more stringent.

          - Repair damaged and deteriorated concrete according to resinous flooring manufacturer's written instructions.

          - Verify that concrete substrates are dry and moisture-vapor emissions are within acceptable levels according to manufacturer's written instructions.

            - Refer to Section 09 05 65 “Preinstallation Testing for Floor Finishes.”

          - Proceed with application only after substrates pass testing and receiving written approval from flooring manufacturer.

        - Resinous Materials:  Mix components and prepare materials according to resinous flooring manufacturer's written instructions.

        - Use patching and fill material to fill holes and depressions in substrates according to manufacturer's written instructions.

        - To prevent cracks from reflecting through resinous flooring, fill control joints and other nonmoving substrate cracks with a semi-rigid sealant according to manufacturer's written instructions.

      - APPLICATION

        - General:  Apply components of resinous flooring system according to manufacturer's written instructions to produce a uniform, monolithic wearing surface of thickness indicated.

          - Coordinate application of components to provide optimum adhesion of resinous flooring system to substrate, and optimum intercoat adhesion.

          - Cure resinous flooring components according to manufacturer's written instructions.  Prevent contamination during application and curing processes.

RETAIN "EXPANSION AND ISOLATION JOINT TREATMENT" SUBPARAGRAPH BELOW FOR EXPANSION OR ISOLATION JOINTS IN FLOOR. RESINOUS FLOORING MAY REQUIRE THAT FLOORING MATERIALS BE PLACED OVER JOINTS, CURED, SAW-CUT, AND THEN RESEALED; VERIFY PROCEDURE WITH MANUFACTURER. DETAIL JOINTS ON DRAWINGS AND REVISE BELOW TO SUIT PROJECT.

          - At substrate expansion and isolation joints, comply with resinous flooring manufacturer's written instructions.

DELETE "PRIMER" PARAGRAPH BELOW IF ONLY SELF-PRIMING SYSTEMS ARE REQUIRED.

        - Apply primer over prepared substrate at manufacturer's recommended spreading rate.

RETAIN "WATERPROOFING MEMBRANE" PARAGRAPH BELOW IF WATERPROOFING MEMBRANE IS REQUIRED. WATERPROOFING MEMBRANES MAY NOT REQUIRE A PRIMER; VERIFY REQUIREMENTS FOR RESINOUS FLOORING SYSTEMS SELECTED.

        - Apply waterproofing membrane, where indicated, in manufacturer's recommended thickness.

          - Apply waterproofing membrane to integral cove base substrates.

RETAIN SUBPARAGRAPH BELOW IF REQUIRED.

        - Apply reinforcing membrane to entire substrate surface.

IN "REINFORCING MEMBRANE" PARAGRAPH BELOW, APPLYING REINFORCING MEMBRANE ONLY TO SUBSTRATE CRACKS MAY BE ADEQUATE FOR AREAS SUBJECT TO MODERATE IMPACT; CONSULT MANUFACTURERS FOR RECOMMENDATIONS. PRIMER MAY NOT BE REQUIRED IF REINFORCING MEMBRANE COVERS ENTIRE SUBSTRATE SURFACE; VERIFY REQUIREMENTS FOR RESINOUS FLOORING SYSTEMS SELECTED.

        - Reinforcing Membrane: Apply reinforcing membrane to [substrate cracks] [entire substrate surface].

RETAIN "INTEGRAL COVE BASE" PARAGRAPH BELOW FOR INTEGRAL COVE BASE. IF RETAINING, INSERT REQUIREMENTS FOR INSTALLING METAL OR PLASTIC COVE CAPS IF REQUIRED.

        - Integral Cove Base:  Apply cove base mix to wall surfaces before applying flooring.  Apply according to manufacturer's written instructions and details including those for taping, mixing, priming, troweling, sanding, and topcoating of cove base.  Round internal and external corners.

          - Integral Cove Base:  4 inches (100 mm) <Insert dimension>high.

RETAIN "SELF-LEVELING BODY COATS" PARAGRAPH BELOW FOR SELF-LEVELING SYSTEMS. IF RETAINING, INDICATE THICKNESS IN PART 2 OR INSERT BELOW.

        - Apply self-leveling slurry body coats in thickness indicated for flooring system.

RETAIN "AGGREGATES" SUBPARAGRAPH BELOW FOR BROADCAST AGGREGATES; REVISE TO SUIT SYSTEMS SELECTED.

          - Broadcast aggregates at rate recommended by manufacturer and, after resin is cured, remove excess aggregates to provide surface texture indicated.

        - Apply topcoats in number indicated for flooring system and at spreading rates recommended in writing by manufacturer.

      - FIELD QUALITY CONTROL

        - Core Sampling:  At the direction of Owner and at locations designated by Owner, take one core sample per 1000 sq. ft. (92.9 sq. m) of resinous flooring, or portion of, to verify thickness.  For each sample that fails to comply with requirements, take two additional samples.  Repair damage caused by coring and correct deficiencies.

        - Material Sampling:  Owner may at any time and any number of times during resinous flooring application require material samples for testing for compliance with requirements.

          - Owner will engage an independent testing agency to take samples of materials being used.  Material samples will be taken, identified, sealed, and certified in presence of Contractor.

          - Testing agency will test samples for compliance with requirements, using applicable referenced testing procedures or, if not referenced, using testing procedures listed in manufacturer's product data.

          - If test results show applied materials do not comply with specified requirements, pay for testing, remove noncomplying materials, prepare surfaces coated with unacceptable materials, and reapply flooring materials to comply with requirements.

      - PROTECTION

        - Protect resinous flooring from damage and wear during the remainder of construction period.  Use protective methods and materials, including temporary covering, recommended in writing by resinous flooring manufacturer.

END OF SECTION 09 67 23

FOR MDACC USE ONLY. DELETE THIS PAGE BEFORE ISSUING DOCUMENTS.

document revision history

| Issue | Date | Revision Description | Author |
| --- | --- | --- | --- |
|  | 20190301 | Original Issuance |  |
| Rev. 1 |  | . |  |
| Rev. 2 |  |  |  |
| Rev. 3 |  |  |  |
| Rev. 4 |  |  |  |
| Rev. 5 |  |  |  |